Project 1

5/26/2014 8:32:22 AM

Too many elements to fit on page ( 8 max. ) Please consider using the copy to clipboard function.

Project 1

5/26/2014 8:32:31 AM

Project: Project 1

Owner: INCA

Site: Site of Interest 1

Sample: Sample 1

Type: Default

ID:

Processing option : All elements analysed (Normalised)

| Spectrum | In stats. | C | O | Na | Al | Si | Cl | K | Ca | Cr | Fe | Zn | Zr |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Spectrum 1 | Yes | 4.85 | 50.55 | 0.57 |  | 20.84 |  |  |  | 0.15 |  |  | 23.03 |  |  |
| Spectrum 2 | Yes | 9.78 | 59.39 | 4.04 | 11.14 | 14.01 | 0.67 | 0.19 | 0.19 |  | 0.25 | 0.34 |  |  |  |
| Max. |  | 9.78 | 59.39 | 4.04 | 11.14 | 20.84 | 0.67 | 0.19 | 0.19 | 0.15 | 0.25 | 0.34 | 23.03 |  |  |
| Min. |  | 4.85 | 50.55 | 0.57 | 11.14 | 14.01 | 0.67 | 0.19 | 0.19 | 0.15 | 0.25 | 0.34 | 23.03 |  |  |

All results in atomic%

Project 1

5/26/2014 8:32:41 AM

Too many elements to fit on page ( 8 max. ) Please consider using the copy to clipboard function.

Project 1

5/26/2014 8:32:58 AM

Project: Project 1

Owner: INCA

Site: Site of Interest 2

Sample: Sample 1

Type: Default

ID:

Processing option : All elements analysed (Normalised)

| Spectrum | In stats. | C | O | Na | Al | Si | P | Cl | K | Ca | Cu | Zr |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Spectrum 1 | Yes | 41.55 | 38.65 | 2.11 |  | 9.24 |  |  |  |  |  | 8.45 |  |  |
| Spectrum 2 | Yes | 68.95 | 17.68 | 1.33 | 0.36 | 3.47 |  |  | 0.09 | 0.25 | 4.51 | 3.35 |  |  |
| Spectrum 3 | Yes |  | 69.36 |  | 14.07 | 16.17 |  | 0.23 | 0.00 | 0.17 |  |  |  |  |
| Spectrum 4 | Yes | 75.81 | 14.89 | 5.54 |  | 0.38 | 1.57 | 0.80 | 0.17 | 0.83 |  |  |  |  |
| Max. |  | 75.81 | 69.36 | 5.54 | 14.07 | 16.17 | 1.57 | 0.80 | 0.17 | 0.83 | 4.51 | 8.45 |  |  |
| Min. |  | 41.55 | 14.89 | 1.33 | 0.36 | 0.38 | 1.57 | 0.23 | 0.00 | 0.17 | 4.51 | 3.35 |  |  |

All results in atomic%

Project 1

5/26/2014 8:33:27 AM

Processing option : All elements analysed (Normalised)

| Spectrum | In stats. | C | O | Na | Si | P | Cl | Ca |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Spectrum 1 | Yes | 63.17 | 19.71 | 6.70 | 1.46 | 1.19 | 3.69 | 4.09 |  |  |
| Mean |  | 63.17 | 19.71 | 6.70 | 1.46 | 1.19 | 3.69 | 4.09 |  |  |
| Std. deviation |  | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 |  |  |
| Max. |  | 63.17 | 19.71 | 6.70 | 1.46 | 1.19 | 3.69 | 4.09 |  |  |
| Min. |  | 63.17 | 19.71 | 6.70 | 1.46 | 1.19 | 3.69 | 4.09 |  |  |

All results in atomic%

Project 1

5/26/2014 8:33:58 AM

Too many elements to fit on page ( 8 max. ) Please consider using the copy to clipboard function.

Project 1

5/26/2014 8:34:06 AM

Project: Project 1

Owner: INCA

Site: Site of Interest 4

Sample: Sample 1

Type: Default

ID:

Processing option : All elements analysed (Normalised)

| Spectrum | In stats. | C | O | Na | Al | Si | P | Cl | Ca | Ti | Fe | Zr |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Spectrum 1 | Yes | 11.28 | 64.22 | 1.31 | 0.58 | 0.78 | 0.00 | 0.31 | 0.73 | 20.32 | 0.47 |  |  |  |
| Spectrum 2 | Yes | 30.53 | 45.91 | 1.20 | 0.72 | 11.13 |  |  | 0.55 |  |  | 9.96 |  |  |
| Spectrum 3 | Yes |  | 67.44 |  | 16.16 | 16.40 |  |  |  |  |  |  |  |  |
| Spectrum 4 | Yes | 5.33 | 58.25 |  | 0.81 | 16.96 |  |  | 0.34 |  |  | 18.32 |  |  |
| Max. |  | 30.53 | 67.44 | 1.31 | 16.16 | 16.96 | 0.00 | 0.31 | 0.73 | 20.32 | 0.47 | 18.32 |  |  |
| Min. |  | 5.33 | 45.91 | 1.20 | 0.58 | 0.78 | 0.00 | 0.31 | 0.34 | 20.32 | 0.47 | 9.96 |  |  |

All results in atomic%

Project 1

5/26/2014 8:34:20 AM

Processing option : All elements analysed (Normalised)

| Spectrum | In stats. | C | O | Si | Ca | Zr |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Spectrum 1 | Yes | 2.09 | 40.20 | 27.19 |  | 30.52 |  |  |
| Spectrum 2 | Yes |  | 64.78 | 16.60 | 0.30 | 18.32 |  |  |
| Max. |  | 2.09 | 64.78 | 27.19 | 0.30 | 30.52 |  |  |
| Min. |  | 2.09 | 40.20 | 16.60 | 0.30 | 18.32 |  |  |

All results in atomic%

Project 1

5/26/2014 8:34:30 AM

Processing option : All elements analysed (Normalised)

| Spectrum | In stats. | C | O | Na | Al | Si | K | Zr |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Spectrum 1 | Yes |  | 60.77 |  | 39.23 |  |  |  |  |  |
| Spectrum 2 | Yes | 1.48 | 60.03 | 4.17 | 7.87 | 24.22 | 2.23 |  |  |  |
| Spectrum 3 | Yes | 3.37 | 68.48 |  | 13.60 | 14.55 |  |  |  |  |
| Spectrum 4 | Yes |  | 57.50 |  |  | 20.02 |  | 22.48 |  |  |
| Max. |  | 3.37 | 68.48 | 4.17 | 39.23 | 24.22 | 2.23 | 22.48 |  |  |
| Min. |  | 1.48 | 57.50 | 4.17 | 7.87 | 14.55 | 2.23 | 22.48 |  |  |

All results in atomic%

Project 1

5/26/2014 8:34:41 AM

Processing option : All elements analysed (Normalised)

| Spectrum | In stats. | C | O | Na | Al | Si | K | Ca | Zr |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Spectrum 1 | Yes | 5.32 | 56.03 |  |  | 17.35 |  |  | 21.29 |  |  |
| Spectrum 2 | Yes | 14.95 | 53.13 | 1.34 | 19.32 | 10.04 | 0.94 | 0.28 |  |  |  |
| Spectrum 3 | Yes |  | 63.44 |  | 3.03 | 17.16 |  |  | 16.36 |  |  |
| Max. |  | 14.95 | 63.44 | 1.34 | 19.32 | 17.35 | 0.94 | 0.28 | 21.29 |  |  |
| Min. |  | 5.32 | 53.13 | 1.34 | 3.03 | 10.04 | 0.94 | 0.28 | 16.36 |  |  |

All results in atomic%

Project 1

5/26/2014 8:34:48 AM

Too many elements to fit on page ( 8 max. ) Please consider using the copy to clipboard function.

Project 1

5/26/2014 8:34:56 AM

Project: Project 1

Owner: INCA

Site: Site of Interest 8

Sample: Sample 1

Type: Default

ID:

Processing option : All elements analysed (Normalised)

| Spectrum | In stats. | C | O | Na | Al | Si | Cl | K | Ca | Zr | Ta |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Spectrum 1 | Yes | 9.46 | 58.91 | 0.91 | 0.90 | 29.83 |  |  |  |  | 0.00 |  |  |
| Spectrum 2 | Yes |  | 64.86 |  |  | 16.29 |  |  |  | 18.85 |  |  |  |
| Spectrum 3 | Yes | 1.19 | 62.79 |  |  | 36.02 |  |  |  |  |  |  |  |
| Spectrum 4 | Yes | 10.18 | 60.96 | 0.46 | 6.53 | 20.35 | 0.33 | 0.59 | 0.60 |  |  |  |  |
| Spectrum 5 | Yes | 8.66 | 61.20 |  | 14.44 | 15.17 |  |  | 0.53 |  |  |  |  |
| Spectrum 6 | Yes |  | 67.12 |  | 15.08 | 17.37 |  |  | 0.43 |  |  |  |  |
| Max. |  | 10.18 | 67.12 | 0.91 | 15.08 | 36.02 | 0.33 | 0.59 | 0.60 | 18.85 | 0.00 |  |  |
| Min. |  | 1.19 | 58.91 | 0.46 | 0.90 | 15.17 | 0.33 | 0.59 | 0.43 | 18.85 | 0.00 |  |  |

All results in atomic%

Project 1

5/26/2014 8:35:08 AM

Processing option : All elements analysed (Normalised)

| Spectrum | In stats. | C | O | Al | Si | Zr |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Spectrum 1 | Yes |  | 56.07 | 17.75 | 26.17 |  |  |  |
| Spectrum 2 | Yes | 3.65 | 42.95 |  | 24.82 | 28.58 |  |  |
| Spectrum 3 | Yes | 4.91 | 65.39 | 14.88 | 14.81 |  |  |  |
| Max. |  | 4.91 | 65.39 | 17.75 | 26.17 | 28.58 |  |  |
| Min. |  | 3.65 | 42.95 | 14.88 | 14.81 | 28.58 |  |  |

All results in atomic%

Project 1

5/26/2014 8:35:16 AM

Processing option : All elements analysed (Normalised)

| Spectrum | In stats. | C | O | Na | Al | Si | Cl | Ca | Zn |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Spectrum 1 | Yes | 3.26 | 62.55 | 1.78 | 16.32 | 15.20 | 0.24 | 0.23 | 0.42 |  |  |
| Spectrum 2 | Yes |  | 61.98 |  |  | 38.02 |  |  |  |  |  |
| Max. |  | 3.26 | 62.55 | 1.78 | 16.32 | 38.02 | 0.24 | 0.23 | 0.42 |  |  |
| Min. |  | 3.26 | 61.98 | 1.78 | 16.32 | 15.20 | 0.24 | 0.23 | 0.42 |  |  |

All results in atomic%

Project 1

5/26/2014 8:35:24 AM

Processing option : All elements analysed (Normalised)

| Spectrum | In stats. | C | O | Al | Si | Zr |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Spectrum 1 | Yes |  | 17.46 |  | 41.56 | 40.98 |  |  |
| Spectrum 2 | Yes |  |  | 6.47 | 53.54 | 39.99 |  |  |
| Spectrum 3 | Yes |  | 38.17 |  | 31.72 | 30.10 |  |  |
| Spectrum 4 | Yes | 27.81 | 46.13 |  | 12.48 | 13.58 |  |  |
| Spectrum 5 | Yes |  | 62.70 |  | 16.82 | 20.47 |  |  |
| Max. |  | 27.81 | 62.70 | 6.47 | 53.54 | 40.98 |  |  |
| Min. |  | 27.81 | 17.46 | 6.47 | 12.48 | 13.58 |  |  |

All results in atomic%

Project 1

5/26/2014 8:35:51 AM

Processing option : All elements analysed (Normalised)

| Spectrum | In stats. | C | O | Al | Si | Ti | Ag |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Spectrum 1 | Yes | 7.67 | 61.04 | 3.10 | 1.22 | 24.40 | 2.57 |  |  |
| Spectrum 2 | Yes |  | 69.75 | 1.75 |  | 28.50 |  |  |  |
| Max. |  | 7.67 | 69.75 | 3.10 | 1.22 | 28.50 | 2.57 |  |  |
| Min. |  | 7.67 | 61.04 | 1.75 | 1.22 | 24.40 | 2.57 |  |  |

All results in atomic%

Project 1

5/26/2014 8:36:00 AM

Too many elements to fit on page ( 8 max. ) Please consider using the copy to clipboard function.

Project 1

5/26/2014 8:36:06 AM

Project: Project 1

Owner: INCA

Site: Site of Interest 13

Sample: Sample 1

Type: Default

ID:

Processing option : All elements analysed (Normalised)

| Spectrum | In stats. | C | O | Na | Mg | Al | Si | K | Ca | Sc | Ta |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Spectrum 1 | Yes |  | 16.80 | 3.13 |  | 15.73 | 55.37 | 8.21 | 0.76 |  |  |  |  |
| Spectrum 2 | Yes | 5.27 | 59.33 | 1.27 |  | 4.60 | 27.41 | 1.76 | 0.37 |  |  |  |  |
| Spectrum 3 | Yes | 21.56 | 52.07 |  | 0.43 | 0.98 | 1.98 |  | 22.23 | 0.75 | 0.00 |  |  |
| Max. |  | 21.56 | 59.33 | 3.13 | 0.43 | 15.73 | 55.37 | 8.21 | 22.23 | 0.75 | 0.00 |  |  |
| Min. |  | 5.27 | 16.80 | 1.27 | 0.43 | 0.98 | 1.98 | 1.76 | 0.37 | 0.75 | 0.00 |  |  |

All results in atomic%